|  |  |  |  |  |  | PROCESS MATERIAL DATA SHEET |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  |  | REV. |
| PROJECT TITLE |  |  |  | 7701 – GELSA, Spain |  |  | PROJECT NO. | 7701 |  |  |  |
| P &ID REF. NO. |  |  |  | - |  |  | DOC. NO. | 7701-C50-TDS-GMT-001 |  |  |  |
| PROCESS AREA |  |  |  | C – Gypsum Dewatering |  |  | SHEET | 1 of 1 |  |  |  |
| PROCESS MATERIAL |  |  |  | Gypsum Slurry |  |  |  |  |  |  |  |
| 1 |  | Basic description: |  |  |  |  |  |  |  |  |  |
|  |  | Slurry: - Gypsum Slurry of Hemi-Hydrate and free water at an approximate ratio of 4.2: 5 (Gypsum to water) on a weight basis. |  |  |  |  |  |  |  |  |  |
| 2 |  | SPECIFICATION (Properties at 85OC): |  |  |  |  |  |  |  |  |  |
|  |  | - APPEARANCE: Milky-white Slurry - BULK DENSITY: Free flowing: ~1,600 Kg/m3 Solids (Settled): 2,700 Kg/m3 Liquid (Filtrate): ~1,000 Kg/m3 - TEMPERATURE, OC: <80-100OC - FLOWABILITY: Temperature dependent, higher temperature greater flowability - ABRASION: Low-medium (depending on temperature/settling factors) - ESTIMATED PARTICLE SIZE DISTRIBUTION (PSD): D10: 16 µm D50: 30 µm D90: 52 µm - pH: 6-7 - CHEMICAL COMPOSITION BY WEIGHT: W/W HEMIHYDRATE: ~45 % W/W FREE WATER: ~54.3 % W/W SUCCINIC ACID: <0.001 % W/W SODIUM: 0.003% W/W CHLORIDE: 0.01% |  |  |  |  |  |  |  |  |  |
| REV |  | DATE |  | DESCRIPTION |  |  |  | BY | APPROVED |  |  |
| A |  | 24/11/2021 |  | First Issue |  |  |  | TE |  |  |  |
| Saint-Gobain Gypsum, Gypsum Engineering, East Leake, Loughborough, LE12 6JS Tel: 0115 945 1600 Fax: 0115 945 1650 |  |  |  |  |  |  |  |  |  |  |  |